| COMPETENCY-BASED CURRICULUM |  |
| --- | --- |

| Sector: METALS AND ENGINEERING |
| --- |
| Qualification: Gas Tungsten Arc Welding (GTAW) NC II |
|  | Technical Education and Skills Development Authority East Service Road, South Superhighway, Taguig City, Metro Manila |

TABLE OF CONTENTS

Page

A. Course Design	1-5

B. Modules of Instruction	6-90

  - BASIC COMPETENCIES

  - Participating in workplace communication	7-10

  - Working in a team environment	11-13

  - Practicing career professionalism	14-17

  - Practicing occupational health and safety	18-22

  - COMMON COMPETENCIES

  - Applying safety practices	24-29

  - Interpreting drawing and sketches	30-33

  - Performing industry calculation	34-38

  - Contributing to quality system	39-42

  - Using hand tools	43-46

  - Preparing weld materials	47-52

  - Setting-up welding equipment	53-56

  - Fitting-up materials	57-59

  - Repairing weld	60-64

  - CORE COMPETENCIES

  - Performing fillet welding on carbon steel plate	66-74

  - Performing groove welding on carbon steel plate	 75-83

  - Performing groove welding on carbon steel pipe	84-90

# COURSE DESIGN

# COURSE TITLE	:	GAS TUNGSTEN ARC WELDING (GTAW) NC II

NOMINAL DURATION	:	268 hours

COURSE DESCRIPTION	:

This course is designed to enhance the knowledge, desirable attitudes and skills of a GTAW welder in accordance with industry standards. It covers core competencies such as; weld carbon steel plates, weld carbon steel pipe using GTAW. This includes common competencies; apply safety practices, interpret drawing and sketches, perform industry calculations, contribute to quality system, use hand tools, prepare weld materials, setup welding equipment, fit up weld materials and repair welds. It also includes competencies such as, participate in workplace communication, work in a team environment, practice career professionalism and practice occupational health and safety procedure.

ENTRY REQUIREMENTS	:

Candidate/trainee must posses any of the following qualifications;

- completed training in SMAW NC II or a holder of SMAW NC II

- can communicate both orally and in written form

- physically  and mentally fit

- can perform basic mathematical computation

COURSE STRUCTURE:

# BASIC COMPETENCIES

(18 hours)

| UNIT OF COMPETENCY | MODULE TITLE | LEARNING OUTCOMES | NOMINAL DURATION |
| --- | --- | --- | --- |
| 1. Participate in workplace communication | 1.1 Participating in workplace communication | 1.1.1 Obtain and convey workplace information 1.1.2 Complete relevant work related documents 1.1.3 Participate in workplace meeting and discussion | 4 hours |
| 2. Work in a team environment | 2.1 Working in a team environment | 2.1.1 Describe and identify team role and responsibility in a team. 2.1.2 Describe work as a team | 4 hours |
| 3. Practice career professionalism | 3.1 Practicing career professionalism | 3.1.1 Integrate personal objectives with organizational goals 3.1.2 Set and meet work priorities 3.1.3 Maintain professional growth and development | 6 hours |
| 4. Practice occupational health and safety | 4.1 Practicing occupational health and safety | Identity hazards and risks 4.1.2 Evaluate hazards and risks 4.1.3 Control hazards and risks 4.1.4 Maintain occupational health and safety awareness | 4 hours |

# COMMON COMPETENCIES

(56 hours)

| UNIT OF COMPETENCY | MODULE TITLE | LEARNING OUTCOMES | NOMINAL DURATION |
| --- | --- | --- | --- |
| Apply safety practices | 1.1 Applying safety practices | Identify hazardous area Use personal protective clothing and devices 1.1.3 Perform safe handling of tools, equipment and materials 1.1.4 Perform first aid 1.1.5 Use Fire extinguisher | 8 hours |
| Interpret drawing and sketches | 2.1 Interpreting drawing and sketches | 2.1.1 Identify standard alphabet of lines 2.1.2 Identify orthographic/ isometric views 2.1.3 Interpret standard drawing symbols, dimensional tolerances and notations | 8 hours |
| Perform industry calculation | 3.1 Performing industry calculation | 3.1.1 Perform four fundamental operations. 3.1.2 Perform conversion of units 3.1.3 Perform calculations on algebraic expressions 3.1.4 Compute percentage and ratio | 8 hours |
| Contribute to quality system | 4.1 Contributing to quality system | 4.1.1 Inspect work done. 4.1.2 Apply quality standards to work 4.1.3 Protect company property and customer interests | 4 hours |
| Use handtools | 5.1 Using handtools | 5.1.1 Select hand tools 5.1.2 Use hand tools 5.1.3 Maintain hand tools | 4 hours |
| Prepare weld materials | 6.1 Preparing weld materials | 6.1.1 Set up cutting equipment 6.1.2 Cut and prepare edge of materials 6.1.3 Clean surfaces and edges 6.1.4 Prepare welding consumables 6.1.5 Prepare welding safety and protective equipment | 8 hours |
| set-up welding equipment | 7.1 Setting-up welding equipment | 7.1.1 Set up welding machine 7.1.2 Set up welding accessories 7.1.3 Set up welding positioners, jigs and fixtures | 4 hours |
| Fit-up materials | 8.1 Fitting up materials | 8.1.1 Perform tack welding 8.1.2 Check gap and alignment | 4 hours |
| Repair weld | 9.1 Repairing weld | 9.1.1 Mark/locate weld defects 9.1.2 Prepare tools and equipment 9.1.3 Remove defects 9.1.4 Perform re-welding | 8 hours |

# CORE COMPETENCIES

(194 hours)

| UNIT OF COMPETENCY | MODULE TITLE | LEARNING OUTCOMES | NOMINAL DURATION |
| --- | --- | --- | --- |
| 1. Weld carbon steel plate using GTAW | Perform fillet welding on carbon steel plate | 1.1.1 Weld carbon steel plates in flat position (IF) 1.1.2 Weld carbon steel plates in horizontal position (2F) 1.1.3 Weld carbon steel plates in vertical position (3F) 1.1.4 Weld carbon steel plates in overhead position (4F) | 50 hours |
|  | Perform groove welding on carbon steel plate | 1.2.1 Weld carbon steel plates in flat position (IG) 1.2.2 Weld carbon steel plates in horizontal position (2G) 1.2.3 Weld carbon steel plates in vertical position (3G) 1.2.4 Weld carbon steel plates in overhead position (4G) | 64 hours |
| 2. Weld carbon steel pipe using GTAW | Perform groove welding on carbon steel pipe | 2.1.1 Weld carbon steel pipes in flat position (2G) 2.1.2 Weld carbon steel pipes in horizontal position (5G) 2.1.3 Weld carbon steel in pipes vertical position (6G) | 80 hours |

# ASSESSMENT METHODS:

- Written examination

- Demonstration of practical skills

- Direct observation

- Interview

COURSE DELIVERY:

- Modular

- Demonstration

- Lecture

- Discussion

- Dual training

- Self-paced learning

RESOURCES:

| Equipment DC welding machine complete with accessories Welding booth Welding table or jig Tools/accessories/supplies Set of box wrench Welding mask Chipping hammer Steel brush Dark glass Clear glass Weld gauge Penlight Dye penetrant (DPT) kit Cutting / grinding disk Carbon steel pipes Filler rod Tungsten electrode Argon Tig torch and accessories Gas flowmeter Portable grinder | Training materials Reference books Manuals Catalogs Brochures Modules/LEs CDs/Video tapes Arc welding manuals Welding standards Welding procedures specifications (WPS) Personal protective equipment Safety shoes Safety goggles Apron Tig gloves Leggings |
| --- | --- |

# QUALIFICATIONS OF INSTRUCTOR:

- Must be a holder of Welding (GTAW) NC II.

- Must have undergone training on Training Methodology II (TM II).

- Must be computer literate.

- Must be physically and mentally fit.

- *Must have at least 2 years job/ industry experience.

- Must be a civil service eligible or appropriate professional license issued by the Professional Regulatory Commission (for government position).

* Optional: only when required by hiring institution

AS PER TESDA RESOLUTION NO. 2004-03

MODULES OF INSTRUCTION

BASIC COMPETENCIES

GAS TUNGSTEN ARC WELDING (GTAW) NC II

UNIT OF COMPETENCY	:	PARTICIPATE IN WORKPLACE COMMUNICATION

MODULE TITLE	:	PARTICIPATING IN WORKPLACE COMMUNICATION

MODULE DESCRIPTOR	: 	This module covers the knowledge, skills and attitudes required to obtain, interpret and convey information in response to workplace requirements.

SUGGESTED DURATION	:	4 hours

PREREQUISITE	:	Receive and Respond to Workplace Communication. (NC I)

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the students/ trainees will be able to:

# LO1.	Obtain and convey workplace information

LO2.	Complete relevant work related documents.

LO3.	Participate in workplace meeting and discussion.

LO1.	OBTAIN AND CONVEY WORKPLACE INFORMATION

ASSESSMENT CRITERIA:

1.	Specific relevant information is accessed from appropriate sources.

2.	Effective questioning, active listening and speaking skills are used to gather and convey information.

3.	Appropriate medium is used to transfer information and ideas.

4.	Appropriate non-verbal communication is used.

5.	Appropriate lines of communication with superiors and colleagues are identified and followed.

6.	Defined workplace procedures for the location and storage of information are used.

7.	Personal interaction is carried out clearly and concisely.

CONTENTS:

- Parts of speech

- Sentence construction

- Effective communication

CONDITIONS:

The students/ trainees must be provided with the following:

- Writing materials (pen & paper)

- References (books)

- Manuals

METHODOLOGIES:

- Group discussion

- Interaction

- Lecture

- Reportorial

ASSESSMENT METHODS:

- Written test

- Practical/performance test

- Interview

L02.	COMPLETE RELEVANT WORK RELATED DOCUMENTS

ASSESSMENT CRTERIA:

1.	Ranges of forms relating to conditions of employment are completed accurately and legibly.

2.	Workplace data is recorded on standard workplace forms and documents.

- Basic mathematical processes are used for routine calculations.

- Errors in recording information on forms/ documents are identified and rectified.

5.	Reporting requirements to superior are completed according to enterprise guidelines.

CONTENTS:

- Basic mathematics

- Technical writing

- Types of forms

CONDITIONS:

The students/trainees must be provided with the following:

- Paper

- Pencils/ball pen

- Reference books

- Manuals

METHODOLOGIES:

- Group discussion

- Interaction

- Lecture

ASSESSMENT METHODS:

- Written test

- Practical/performance test

- Interview

LO3.	PARTICIPATE IN WORKPLACE MEETINGS AND DISCUSSIONS

ASSESSMENT CRITERIA:

1.	Team meetings are attended on time.

2.	Own opinions are clearly expressed and those of others are listened to without interruption.

3.	Meeting inputs are consistent with the meeting purpose and established protocols.

4.	Workplace interaction are conducted in a courteous manner appropriate to cultural background and authority in the enterprise procedures.

5.	Questions about simple routine workplace procedures and matters concerning conditions of employment are asked and responded.

6.	Meeting outcomes are interpreted and implemented.

CONTENTS:

- Sentence construction

- Technical writing

- Recording information

CONDITIONS:

The students/trainees must be provided with the following:

- Paper

- Pencils/ball pen

- References (books)

- Manuals

METHODOLOGIES:

- Group discussions

- Interaction

- Lecture

ASSESSMENT METHODS:

- Written test

- Practical/performance test

- Interview

UNIT OF COMPETENCY	:	WORK IN A TEAM ENVIRONMENT

MODULE TITLE	:	WORKING IN A TEAM ENVIRONMENT

MODULE DESCRIPTOR	:	This module covers the knowledge, skills, and attitudes required to relate in a work based environment.

SUGGESTED DURATION	:	4 hours

QUALIFICATION LEVEL	: 	NC II

PREREQUISITE	:	TEAMWORK (NC I)

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module, the students/ trainees will be able to:

LO1.	Describe and identify team role and responsibility in a team.

LO2.	Describe work as a team.

LO1.	DESCRIBE AND IDENTIFY TEAM ROLE AND RESPONSIBILITY IN A TEAM

ASSESSMENT CRITERIA:

1.	Role and objective of the team is identified.

2.	Team parameters, relationships and responsibilities are identified.

3.	Individual role and responsibilities within team environment are identified.

4.	Roles and responsibilities of other team members are identified and recognized.

5.	Reporting relationships within team and external to team are identified.

CONTENTS:

- Team role.

- Relationship and responsibilities

- Role and responsibilities with team environment.

- Relationship within a team.

CONDITIONS:

The students/ trainees must be provided with the following:

- Standard operating procedure (SOP) of workplace

- Job procedures

- Client/supplier instructions

- Quality standards

- Organizational or external personnel

METHODOLOGIES:

- Group discussion/interaction

- Case studies

- Simulation

ASSESSMENT METHODS:

- Written test

- Observation

- Simulation

- Role playing

LO2.	DESCRIBE WORK AS A TEAM MEMBER

ASSESSMENT CRITERIA:

1.	Appropriate forms of communication and interactions are undertaken.

2.	Appropriate contributions to complement team activities and objectives were made.

3.	Reporting using standard operating procedures followed.

4.	Development of team work plans based from role team were contributed.

CONTENTS:

- Communication process

- Team structure/team roles

- Group planning and decision making

CONDITIONS:

The students/trainees must be provided with the following:

- SOP of workplace

- Job procedures

- Organization or external personnel

METHODOLOGIES:

- Group discussion/interaction

- Case studies

- Simulation

ASSESSMENT METHODS:

- Observation of work activities

- Observation through simulation or role play

- Case studies and scenarios.

UNIT OF COMPETENCY	:	PRACTICE CAREER PROFESSIONALISM

MODULE TITLE	: 	PRACTICING CAREER PROFESSIONALISM

MODULE DESCRIPTOR	: 	This module covers the knowledge, skills and attitudes in promoting career growth and advancement, specifically to integrate personal objectives with organizational goals set and meet work priorities and maintain professional growth and development.

NOMINAL DURATION	:	6 hours

CERTIFICATE LEVEL	: 	NC II

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module, the trainee/student must be able to:

LO1.	Integrate personal objectives with organizational goals

LO2.	Set and meet work priorities

LO3.	Maintain professional growth and development

LO1.	INTEGRATE PERSONAL OBJECTIVES WITH ORGANIZATIONAL GOALS

ASSESSMENT CRITERIA:

1.	Personal growth and work plans towards improving the qualifications set for professionalism are evident.

2.	Intra and interpersonal relationship in the course of managing oneself based on performance evaluation is maintained.

3.	Commitment to the organization and its goal is demonstrated in the performance of duties.

4.	Practice of appropriate personal hygiene is observed.

5.	Job targets within key result areas are attained.

CONTENTS:

- Personal development-social aspects: intra and interpersonal development

- Organizational goals

- Personal hygiene and practices

- Code of ethics

CONDITIONS:

The students/ trainees must be provided with the following:

- Workplace

- Code of ethics

- Organizational goals

- Hand outs and Personal development-social aspects

- CD’s, VHS tapes, transparencies

METHODOLOGIES:

- Interactive -lecture

- Simulation

- Demonstration

- Self paced instruction

ASSESSMENT METHODS:

- Role play

- Interview

- Written examination

LO2.	SET AND MEET WORK PRIORITIES

ASSESSMENT CRITERIA:

1.	Competing demands to achieve personal, team and organizational goals and objectives are prioritized.

2.	Resources are utilized efficiently and effectively to manage work priorities and commitments.

3.	Practices and economic use and maintenance of equipment and facilities are followed as per established procedures.

4.	Job targets within key result areas are attained.

CONTENTS:

- Organizational Key Result Areas (KRA)

- Work values and ethical standards

- Company policies on the use and maintenance of equipment

CONDITIONS:

The students/ trainees must be provided with the following

- Hand outs on

-	Organizational KRA

-	Work values and ethics

-	Company policies and standards

-	Sample job targets

- Learning guides

- CD’s, VHS tapes, transparencies

METHODOLOGIES:

- Interactive lecture

- Group discussion

- Structured activity

- Demonstration

ASSESSMENT METHODS:

- Role play

- Interview

- Written examination

LO3.	MAINTAIN PROFESSIONAL GROWTH AND DEVELOPMENT

ASSESSMENT CRITERIA:

1.	Training and career opportunities relevant to the job requirements are identified and availed.

2.	Licenses and/or certifications according to the requirements of the qualifications are acquired and maintained

3.	Fundamental rights at work including gender sensitivity are manifested/ observed

4.	Training and career opportunities based on the requirements of industry are completed and updated.

CONTENTS:

- Qualification standards

- Gender and development (GAD) sensitivity

- Professionalism in the workplace

- List of professional licenses

CONDITIONS:

## The students/trainees must be provided with the following

- Quality standards

- GAD handouts

- CD’s, VHS tapes on professionalism in the workplace

- Professional licenses samples

METHODOLOGIES:

- Interactive lecture

- Film viewing

- Role play/simulation

- Group discussion

ASSESSMENT METHODS:

- Demonstration

- Interview

- Written examination

- Portfolio assessment

UNIT OF COMPETENCY	:	PRACTICE OCCUPATIONAL HEALTH AND SAFETY PROCEDURES

MODULE TITLE	:	PRACTICING OCCUPATIONAL HEALTH AND SAFETY PROCEDURES

MODULE DESCRIPTOR	:	This module covers the knowledge, skills and attitudes required to comply with the regulatory and organizational requirements for occupational health and safety such as identifying, evaluating and maintaining occupational health and safety (OHS) awareness.

NOMINAL DURATION	:	4 hours

CERTIFICATE LEVEL	:	NC II

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module, the trainee/student must be able to:

LO1.	Identity hazards and risks

LO2.	Evaluate hazards and risks

LO3.	Control hazards and risks

LO4.	Maintain occupational health and safety awareness

LO1.	IDENTIFY HAZARDS AND RISKS

ASSESSMENT CRITERIA:

1.	Workplace hazards and risks are identified and clearly explained.

2.	Hazards/risks and its corresponding indicators are identified in with the company procedures.

3.	Contingency measures are recognized and established in accordance with organizational procedures.

CONTENTS:

- Hazards and risks identification and control

- Organizational safety and health protocol

- Threshold limit value (TLV)

- OHS indicators

CONDITIONS:

The students/ trainees must be provided with the following:

- Workplace

- Personal protective equipment (PPE)

- Learning guides

- Hand-outs

-	Organizational safety and health protocol

-	OHS indicators

-	Threshold limit value

-	Hazards/risk identification and control

- CD’s, VHS tapes, transparencies

METHODOLOGIES:

- Interactive -lecture

- Simulation

- Symposium

- Group dynamics

ASSESSMENT METHODS:

- Situation analysis

- Interview

- Practical examination

- Written examination

# LO2.	EVALUATE HAZARDS AND RISKS

ASSESSMENT CRITERIA:

1.	Terms of maximum tolerable limits are identified based on threshold limit values (TLV)

2.	Effects of hazards are determined.

3.	OHS issues and concerns are identified in accordance with workplace requirements and relevant workplace OHS legislation.

CONTENTS:

- TLV table

- Philippine OHS standards

- Effects of hazards in the workplace

- Ergonomics

- ECC Regulations

CONDITIONS:

## The students/trainees must be provided with the following

- Hand outs on

-	Philippine OHS standards

-	Effects of hazards in the workplace

-	Ergonomics

-	ECC regulations

- TLV table

- CD’s, VHS tapes, transparencies

METHODOLOGIES:

- Interactive lecture

- Situation analysis

- Symposium

- Film viewing

- Group dynamics

ASSESSMENT METHODS:

- Interview

- Written examination

- Simulation

LO3.	CONTROL HAZARDS AND RISKS

ASSESSMENT CRITERIA:

1.	OHS procedures for controlling hazards and risk are strictly followed.

2.	Procedures in dealing with workplace accidents, fire and emergencies are followed in accordance with the organization’s OHS policies.

3.	Personal protective equipment (PPE) is correctly used in accordance with organization’s OHS procedures and practices.

4.	Procedures in providing appropriate assistance in the event of workplace emergencies are identified in line with the established organizational protocol.

CONTENTS:

- Safety regulations

-	Clean air act

-	Electrical and fire safety code

-	Waste management

-	Disaster preparedness and management

- Contingency measures and procedures

CONDITIONS:

The students/trainees must be provided with the following:

- Hand outs on

-	Safety Regulations

-	Clean air act

-	Electrical and fire safety code

-	Waste management

-	Disaster preparedness and management

-	Contingency measures and procedures

- OHS personal records

- PPE

- CD’s, VHS tapes, transparencies

METHODOLOGIES:

- Interactive lecture

- Symposium

- Film viewing

- Group dynamics

- Self-paced instruction

ASSESSMENT METHODS:

- Written examination

- Interview

- Case/situation analysis

- Simulation

LO4.	MAINTAIN OCCUPATIONAL HEALTH AND SAFETY AWARENESS

ASSESSMENT CRITERIA:

1.	Procedures in emergency related drill are strictly followed in line with the established organization guidelines and procedures.

2.	OHS personal records are filled up in accordance with workplace requirements.

3.	PPEs are maintained in line with organization guidelines and procedures.

CONTENTS:

- Operational health and safety procedure, practices and regulations

- Emergency-related drills and training

CONDITIONS:

## The students/trainees must be provided with the following

- Workplace

- PPE

- OHS personal records

- CD’s, VHS tapes, transparencies

- Health record

METHODOLOGIES:

- Interactive lecture

- Simulation

- Symposium

- Film viewing

- Group dynamics

ASSESSMENT METHODS:

- Demonstration

- Interview

- Written examination

- Portfolio assessment

MODULES OF INSTRUCTION

COMMON COMPETENCIES

GAS TUNGSTEN ARC WELDING (GTAW) NC II

UNIT OF COMPETENCY	: 	APPLY SAFETY PRACTICES

# MODULE TITLE	:	Applying safety practices

MODULE DESCRIPTION	: 	This module covers safety practices applied in the workplace.

SUGGESTED DURATION	:	4 hours

SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

### LO1.	Identify hazardous area

### LO2.   Use personal protective clothing and devices

### LO3.	Perform safe handling of tools, equipment and materials

### LO4.	Perform first aid

### LO5.	Use Fire extinguisher

LO1.	IDENTIFY HAZARDOUS AREA

### ASSESSMENT CRITERIA:

- Hazards are identified correctly in accordance with OHS procedures.

- Safety signs and symbols are identified and adhered to in accordance with workplace safety procedure.

### CONTENTS:

  - Hazard to be avoided in welding

  - Welding safety signs and symbols

  - Occupational safety standards and enterprise safety policies.

### CONDITION:

The students/ trainee should be provided with:

  - Safety sign and symbols

  - Instructional materials

-	Reference book

-	Learning modules/manuals

-	Safety standards manual

-	Enterprise safety policies/guidelines

### METHODOLOGIES:

  - Lecture/demonstrations

  - Self pace learning

  - Group discussion

### ASSESSMENT METHODS:

  - Written/oral

  - Direct observation

  - Interview

### LO2.	USE PERSONAL PROTECTIVE CLOTHING AND DEVICES

### ASSESSMENT CRITERIA:

- Personal protective clothing/equipment (PPE) identified as per job requirements

- Proper wearing of PPE are properly observed in accordance with workplace safety policies.

- PPE conformed with the approved occupational safety standards.

### CONTENTS:

- Personal protective equipment (PPE) for different welding operations

- Proper uses of different types of personal protective equipment (PPE)

- Occupational safety standards and enterprise safety policies.

### CONDITION:

### The students/ trainee should be provided with:

- Personal protective equipment (PPE)

-	Hard hat

-	Safety shoes

-	Gloves

-	Goggles

-	Welder apron

- Instructional materials for:

-	Reference book

-	Learning modules/manuals

-	Safety standards

-	Enterprise safety policies/guidelines

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

### LO3.	PERFORM SAFE HANDLING OF TOOLS, EQUIPMENT AND MATERIALS

### ASSESSMENT CRITERIA:

- Pre-use checking and inspection of tools and equipment are conducted in accordance with industry/ company policies.

- Safe handling of tools, equipment and materials are properly observed in accordance with OHS requirements and industry/ company policies.

- Safety label and tag of tools and equipment are strictly followed in accordance with industry/ company policies.

### CONTENTS:

- Pre-use inspection and checking procedure

- Safe handling of tools, equipment and materials

- Equipment and power tools orientation and familiarization

- Workplace Occupational Health and Safety procedures

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/accessories

-	Hard hat

- 	Safety shoes

- 	Gloves

- 	Goggles

- 	Welder apron

- Instructional materials:

-	Reference book

-	Learning modules/manuals

-	Safety standards

-	Enterprise safety policies/guidelines

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

### LO4.	PERFORM FIRST AID

### ASSESSMENT CRITERIA:

- First aid treatment of injuries are carried out according to recommended procedures

- Emergency hotline and proper authority are accessed and contacted in accordance with workplace procedure.

### CONTENTS:

- Different types of injuries

- First aid treatment procedure

- Emergency hotline number and offices

- Proper handling of injured individual

### CONDITION:

### The students/ trainee should be provided with:

- Equipment

-	First aid kit (different types)

-	Oxygen

-	Stretcher

-	Medicine

- Learning materials

-	Video tape, CD’s, transparencies

- Directory hotline number and offices

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO5.	USE FIRE EXTINGUISHER

### ASSESSMENT CRITERIA:

- Fire fighting equipment identified according to types/source of fires.

- Use of fire fighting equipment demonstrated in accordance with manufacturer’s instructions.

- Used fire fighting equipment and accessories are recorded/reported for replacement/refill in accordance with enterprise approved safety regulations.

### CONTENTS:

- Types of fire fighting equipment

- Types of fire extinguishers

- Fire hoses

- Fire hydrants

- Sources/causes of fires

- Proper use of fire fighting equipment

### CONDITION:

### The students/ trainee should be provided with:

- Equipment

-	Fire extinguishers (different types)

-	Fire hydrants

-	Video players/monitors

- Learning materials

-	Types of fires/sources

-	Types of fire fighting equipment and its operations

-	Manuals on fire protection regulations

-	Video tape, CD’s, transparencies

-	Report cards/checklist

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

UNIT OF COMPETENCY	: 	INTERPRET DRAWINGS AND SKETCHES

# MODULE TITLE	:  	Interpreting drawing and sketches

MODULE DESCRIPTION	:	This module covers knowledge, skills and attitudes required to interpret drawing and sketches in accordance with work plan specifications.

### SUGGESTED DURATION	:	8 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Identify standard alphabet of lines

LO2.	Identify orthographic/ isometric views

LO3.   Interpret standard drawing symbols, dimensional tolerances and notations

LO1.	IDENTIFY STANDARD ALPHABET OF LINES

### ASSESSMENT CRITERIA:

- Alphabet of lines identified according to ISO.

2.	Alphabet of lines are clearly explained according to their use.

### CONTENTS:

- Alphabet of lines and applications

- Drawing specifications

- Dimensions

- Scaling

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/accessories

-	OHP/transparencies

-	Computer

-	Video/multi-media materials

- Training materials

-	Reference book,

-	Learning modules

-	Blueprint (sample)

-	Writing instrument

-	Drawing instrument

### METHODOLOGIES:

- Lecture/demonstrations

- Self-paced instruction

- Presentation

### ASSESSMENT METHODS:

- Written

- Direct observation

- Interview/oral

### LO2.	IDENTIFY ORTHOGRAPHIC/ ISOMETRIC VIEWS

### ASSESSMENT CRITERIA:

- Orthographic and isometric views are clearly explained

- Orthographic and isometric drawing are identified based on plan

### CONTENTS:

- Types of welding joints and symbols

- Welding positions, codes and plan specifications

- Contour symbols

- Drawing technique

- Perspective

  - Exploded view

  - Hidden view technique

- Projections

  - First angle projections

  - Third angle projections

### CONDITION:

The students/ trainee should be provided with:

- Equipment/accessories

-	OHP/transparencies

-	Computer

-	Video/multi-media materials

- Training materials

-	Reference book,

-	Learning modules

-	Blueprint (sample)

-	Writing instrument

-	Drawing instrument

### METHODOLOGIES:

- Lecture/demonstrations

- Self-paced instruction

- Presentation

### ASSESSMENT METHODS:

- Written

- Direct observation

- Interview/oral

### LO3.	INTERPRET STANDARD DRAWING SYMBOLS, DIMENSIONAL TOLERANCES

### AND NOTATIONS

### ASSESSMENT CRITERIA:

- Drawing symbols are interpreted according to drawing standards

- Dimensional tolerances, notations are interpreted according to specifications

### CONTENTS:

- Types of welding joints and symbols

- Welding positions, codes and plan specifications

- Contour symbols

- Welding process (abbreviation)

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/accessories

-	OHP/transparencies

-	Computer

-	Video/multi-media materials

- Training materials

-	Reference book,

-	Learning modules

-	Blueprint (sample)

-	Writing instrument

-	Drawing instrument

### METHODOLOGIES:

- Lecture/demonstrations

- Self-paced instruction

- Presentation

### ASSESSMENT METHODS:

- Written

- Direct observation

- Interview/oral

UNIT OF COMPETENCY	:  	PERFORM INDUSTRY CALCULATION

# MODULE TITLE	: 	Performing Industry Calculation

MODULE DESCRIPTION	: 	This module covers knowledge, skill and attitude required to compute/calculate quantity /size/cost of materials/parts, and convert systems of measurements using formulas and other methods.  This also includes measuring instruments and its applications.

SUGGESTED DURATION	:	8 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Perform four fundamental operations.

LO2.	Perform conversion of units

LO3.	Perform calculations on algebraic expressions

LO4.	Compute percentage and ratio

### LO1.	PERFORM FOUR FUNDAMENTAL OPERATION

### ASSESSMENT CRITERIA:

### Simple calculations involving whole numbers, mixed numbers, fraction and decimal are performed using four fundamental operations

### CONTENTS:

- Mathematical operations

- subtraction

- addition

- multiplication

- division

- Industrial mathematics

- Computation formulas finding areas of:

- plane

- circles

- triangles

- other geometrical figures

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/ accessories

-	Calculators

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	PERFORM CONVERSION UNIT

### ASSESSMENT CRITERIA:

1.	Units are converted to the required figure using the given formulae

#### 2.	English measurements are converted to metric measurements according to procedure.

### CONTENTS:

- Units

-	Fractions

-	Mixed numbers

-	Decimal

- Conversion of English to metric (vise versa)

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/ accessories

-	Calculators

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO3.	PERFORM CALCULATIONS ON ALGEBRAIC EXPRESSIONS

### ASSESSMENT CRITERIA:

      - Simple calculations are performed on algebraic expressions using the four fundamental operations

      - Simple transposition of formulae are carried out to isolate the variable required, involving the four fundamental operations.

      - Appropriate formula applied and results obtained in accordance with job specifications.

### CONTENTS:

- English and metric system of measurements

- Four fundamental operations

- Method of transposing formulae

- Equation formulation

### CONDITION:

### The students/ trainee should be provided with:

- Equipment/ accessories

-	Calculators

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO4.	COMPUTE PERCENTAGE AND RATIO

### ASSESSMENT CRITERIA:

1.	Percentages are computed using appropriate formula.

2.	Ratio and proportion are computed using appropriate formula.

### CONTENTS:

- Ratio and proportion

- Calculation

- Percentage and ratio

### CONDITION:

### The students/ trainee should be provided with:

- Equipment /accessories

-	Calculators

- Supplies/materials

-	Pencil/paper

-	Reference books

-	Learning materials/module

-	OHP/transparencies

-	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

UNIT OF COMPETENCY	:  	CONTRIBUTE TO QUALITY SYSTEM

# MODULE TITLE	: 	Contributing to quality system

MODULE DESCRIPTION	: 	This modules covers knowledge, skill and attitude required to inspect work against specification and standards and apply quality standards to work.

SUGGESTED DURATION	:	4 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Inspect work done.

LO2.	Apply quality standards to work

LO3.	Protect company property and customer interests

### LO1.	INSPECT WORK DONE

### ASSESSMENT CRITERIA:

        - Appropriate inspections are conducted to ensure company quality systems and procedures are maintained/ followed.

2.	Job specifications/work order and quality standards are identified.

3.	Faults/defects are identified and rectified according to company procedures.

### CONTENTS:

- Quality system and procedures

-	Work instructions

-	Safe work procedures

-	Product specifications

-	Equipment maintenance schedules

-	Technical procedures adopted or specifically prepared standards

-	Company/industry rules

- Faults and defects

- Communication/feedback methods-written and verbal

### CONDITION:

### The students/ trainee should be provided with:

- Inspection record manual

- Job specification

- Workplace/company procedure manual

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	APPLY QUALITY STANDARDS TO WORK

### ASSESSMENT CRITERIA:

- Inspections are conducted throughout the manufacturing processes to ensure quality standards are maintained.

- Appropriate quality standards are applied throughout the production/fabrication process.

- All activities are coordinated throughout the workplace to ensure efficient quality work outcomes.

### Records of work quality are maintained according to the company requirements

### CONTENTS:

- Quality standard/ISO

- Work inspection techniques/procedures

- Record maintenance

- Communication process

### CONDITION:

### The students/ trainee should be provided with:

- Inspection record manual

- Quality standard

- Job specification

- Workplace/company procedure manual

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO3.	PROTECT COMPANY PROPERTY AND CUSTOMER INTERESTS

### ASSESSMENT CRITERIA:

  - Possible damage to company property is avoided by adherence to company quality procedures.

  - Quality of work is reviewed to ensure customer requirements and company standards are met.

### CONTENTS:

- Company systems, processes and work quality requirements

- Quality assurance principles

- Safety precautionary measures

- Handling materials, tools and equipment

### CONDITION:

The students/ trainee should be provided with:

- Inspection record manual

- Quality standard

- Job specification

- Workplace/company procedure manual

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

UNIT OF COMPETENCY	:	USE HAND TOOLS

# MODULE TITLE                 :	Using hand tools

MODULE DESCRIPTION	:	This modules covers knowledge skills and attitude required to use hand tools

SUGGESTED DURATION	:	4 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Select hand tools

LO2.	Use hand tools

LO3.	Maintain hand tools

### LO1.	SELECT HAND TOOLS

### ASSESSMENT CRITERIA:

- Hand tools selected are appropriate to the requirements of the task.

### Unsafe or defective tools are identified and marked for repair according to procedure

### CONTENTS:

- Types and uses of hand tools

- Hand tool defects

### CONDITION:

### The students/ trainee should be provided with:

- Hand tools

  - Hacksaws

  - Hammers (ball peen, chipping)

  - Punches

  - Screwdrivers

  - Wrenches

  - Scrapers

  - Chisels

  - Gouges

  - Files

  - Clamps

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	USE HAND TOOLS

### ASSESSMENT CRITERIA:

    - Hand tools are used to produce the desired outcomes to job specifications.

### Task performed in accordance with company or industry safety procedure

### CONTENTS:

- Types and uses of hand tools

- Tasks:

- Adjusting

- Dismantling

- Assembling

- Finishing of item or components

### CONDITION:

### The students/ trainee should be provided with:

- Hand tools

  - Hacksaws

  - Hammers (ball peen, chipping)

  - Punches

  - Screwdrivers

  - Wrenches

  - Scrapers

  - Chisels

  - Gouges

  - Files

  - Clamps

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO3.	MAINTAIN HAND TOOLS

### ASSESSMENT CRITERIA:

  - Routine maintenance of hand tools is undertaken according to standard operating procedures, principles and techniques.

  - Hand tools are stored in designated location in accordance with manufacturer’s instruction/standard operating procedure.

### CONTENTS:

- Routine maintenance

  - Lubricating

  - Tightening

  - Simple tool repair

  - Hand sharpening

  - Cleaning

- Proper storage of hand tools

### CONDITION:

### The students/ trainee should be provided with:

- Hand tools

  - Hacksaws

  - Hammers (ball peen, chipping)

  - Punches

  - Screwdrivers

  - Wrenches

  - Scrapers

  - Chisels

  - Gouges

  - Files

  - Clamps

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

UNIT OF COMPETENCY	:	PREPARE WELD MATERIALS

# MODULE TITLE                 :	Preparing weld materials

MODULE DESCRIPTION	: 	This modules covers knowledge, skills and attitude required in preparing weld materials.

SUGGESTED DURATION	:	8 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Set up cutting equipment

LO2.	Cut and prepare edge of materials

LO3.	Clean surfaces and edges

LO4.	Prepare welding consumables

LO5.	Prepare welding safety and protective equipment

### LO1.	SET UP CUTTING EQUIPMENT

### ASSESSMENT CRITERIA:

- Cutting equipment should be operational and should conform to acceptable OH&S standards

- Cutting equipment fittings, connection and power source are checked in accordance with workplace procedure

### CONTENTS:

- Parts and function of cutting equipment

- Procedures in setting–up of cutting equipment

- Procedure in checking cutting equipment functionality.

### CONDITION:

### The students/ trainee should be provided with:

- Hand tools

- Cutting equipment and accessories

- Gases (oxygen, acetylene, LPG)

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	CUT AND PREPARE EDGE OF MATERIALS

### ASSESSMENT CRITERIA:

- Materials are cut to specified dimension/specifications.

- Task are performed in accordance with company/industry requirement and safety procedure

### CONTENTS:

- Cutting operation procedure

- Cutting material with different process

-	Oxy-acetylene gas cutting equipment (manual and automatic)

-	Plasma cutting equipment

-	Shearing machine

-	Disc cutter

-	Cutting electrode

CONDITION:

The students/ trainee should be provided with:

- Hand tools

- Cutting equipment and accessories

- Gases (oxygen, acetylene, LPG)

- Air compressor

- Shearing machine

- Disc cutter

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

### LO3.	PREPARE WELDING CONSUMABLES

ASSESSMENT CRITERIA:

  - Consumables, materials, specified and quantity determined in accordance with job requirements.

  - Correct materials selected in accordance with job requirements.

CONTENTS:

- Consumable materials specifications

- Equipment and tools for preparing plates and pipes edges

- Safe working practices in preparing consumables

CONDITION:

The students/ trainee should be provided with:

- Hand tools

- Cutting equipment and accessories

- Gases (oxygen, acetylene, LPG)

- Air compressor

- Shearing machine

- Disc cutter

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

### LO4.	CLEAN SURFACES AND EDGES

ASSESSMENT CRITERIA:

  - Surfaces are cleaned to required specifications.

  - Task performed in accordance with company or industry requirements and safety procedure

CONTENTS:

- Procedures and techniques of preparing plates and pipe edges for welding

- Equipment and tools for preparing plates and pipes edges

- Safe working practices

CONDITION:

The students/ trainee should be provided with:

- Hand tools

- Cutting equipment and accessories

  - Mild steel

  - Carbon steel

  - Alloy steel

  - Cutting gases

  - Gouging electrodes

  - Grinding/cutting discs

  - Run on/run off, backing plates/ring

- Shearing machine

- Disc cutter

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

### LO5.	PREPARE WELDING SAFETY AND PROTECTIVE EQUIPMENT

ASSESSMENT CRITERIA:

  - PPE should conform to acceptable OH&S requirement and standards.

  - Welding safety and protective equipment are checked in accordance with safety procedure

CONTENTS:

- Procedures and techniques in checking protective equipment

- Safe working practices and handling of protective equipment

CONDITION:

The students/ trainee should be provided with:

- Personal protective equipment

- Supplies/materials

-  	Pencil/paper

-  	Reference books

-  	Learning materials/module

-  	OHP/transparencies

-  	Video/multi-media materials

METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Demonstration

# UNIT OF COMPETENCY	:	SET-UP WELDING EQUIPMENT

# MODULE TITLE                 : 	SETTING-UP WELDING EQUIPMENT

MODULE DESCRIPTION	:	This modules covers knowledge, skills and attitude required in setting up welding   equipment.

SUGGESTED DURATION	:	4 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Set up welding machine

LO2.	Set up welding accessories

LO3.	Set up welding positioners, jigs and fixtures

LO1.	SET UP WELDING MACHINE

### ASSESSMENT CRITERIA:

- Primary cable attached to welding machine primary cable terminal

- Primary cable attached to power source.

- Welding machine checked for functionality.

- Polarity switch, if any, set to DC reverse.

- Cable terminals checked for tightness.

### CONTENTS:

- Parts and function of welding machine  (SMAW)

- Procedures in setting –up of welding machines

- Procedure in checking welding machine functionality.

### CONDITION:

The students/ trainee should be provided with:

- Equipment and accessories

-	AC/DC Welding machine

-	Welding cables

- Ground clamp

-	Primary cable

- Power source  connectors and outlets

- Tools

-	Set of screw driver

-	Set of wrenches

- Supplies/materials

- 	Electrical tape

-  	Rubber tape

- Instructional  materials

-	Reference book /modules/ learning guides/ video CDs

- 	Equipment manual

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO2.	SET UP WELDING ACCESSORIES

### ASSESSMENT CRITERIA:

    - Electrode cable connected to positive of welding machine.

    - Ground cable connected to negative terminal of welding machine.

    - Ground clamp attached to workpiece/material.

    - Welding cable checked for crack, burns and cuts.

    - Primary cable attached to welding machine primary cable terminal

### CONTENTS:

- Parts and function of welding machine accessories and consumables

- Procedures in setting-up of welding accessories

- Procedure in checking welding machine functionality.

### CONDITION:

### The students/ trainee should be provided with:

- Equipment and accessories

-	AC/DC Welding machine

-	Welding cables

- Ground clamp

-	Primary cable

- Power source connectors and outlets

- Tools

-	Set of screw driver

-	Set of wrenches

- Supplies/Materials

- 	Electrical tape

-	Rubber tape

- Instructional  materials

-	Reference book /modules/ learning guides/ video CDs,

- 	Equipment manual

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

### LO3.	SET UP WELDING POSITIONER, JIGS AND FIXTURES

### ASSESSMENT CRITERIA:

  - Braces, stiffeners, rails and other jigs are provided and in conformity with job requirements.

  - Work items/materials are protected from strong winds, drafts and rainfall

### CONTENTS:

- Types of welding positioner, jigs and fixture

- Different kind of jigs and fixture

- Uses and function of welding positioner, jigs and fixture

### CONDITION:

The students/ trainee should be provided with:

- Welding positioner

- Jigs and fixture

- Tools

- Supplies/materials

- Instructional  materials

-	Reference book /modules/ learning guides/ video CDs,

- 	Equipment manual

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

# UNIT OF COMPETENCY	:	FIT UP WELD MATERIALS

# MODULE TITLE                 : 	FITTING UP WELD MATERIALS

MODULE DESCRIPTION	:	This modules covers knowledge, skills and attitude required in fitting up weld materials.

SUGGESTED DURATION	:	4 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Perform tack welding

LO2.	Check gap and alignment

### LO1.	PERFORM TACK WELDING

### ASSESSMENT CRITERIA:

- Tack welding is performed in accordance with the welding procedure requirements

- Joints are free from rust, paints, grease and other foreign materials prior to fit up or tacking.

### CONTENTS:

- Kind of tacking

- Welding procedure standard requirement

- Codes and specification

### CONDITION:

### The students/ trainee should be provided with:

- Welding machine equipment and accessories

  - Tools

  - Supplies/materials

  - Personal protective equipment

  - Drawing plan and specification

  - Instructional  materials

-	Reference book/ modules/ learning guides/ video CDs

- 	Equipment manual

### METHODOLOGIES:

  - Lecture/demonstrations

  - Self pace learning

  - Group discussion

### ASSESSMENT METHODS:

  - Written/oral

  - Direct observation

  - Interview

  - Demonstration

### LO2.	CHECK GAP AND ALIGNMENT

### ASSESSMENT CRITERIA:

  - Root gap is prepared/checked in accordance with WPS  requirements

  - Alignment of work piece are checked in accordance with welding standard

  - Included angle are checked in accordance with WPS

### CONTENTS:

- Fit up tolerances

- Workpiece alignment procedure

- Fit up

### CONDITION:

The students/ trainee should be provided with:

- Measuring tools

- Work piece

- Personal protective equipment

- Drawing plan and specification

- Instructional  materials

-	Reference book /modules/ learning guides/ video CDs,

- 	Equipment manual

### METHODOLOGIES:

- Lecture/demonstrations

- Self pace learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Interview

- Demonstration

# UNIT OF COMPETENCY	:	REPAIR WELD

# MODULE TITLE                 : 	REPAIRING WELD

MODULE DESCRIPTION	:	This modules covers knowledge, skills and attitude required in repairing weld.

SUGGESTED DURATION	:	8 hours

### SUMMARY OF LEARNING OUTCOMES:

At the completion of the module the trainees/students must be able to:

LO1.	Mark/locate weld defects

LO2.	Prepare tools and equipment

LO3.	Remove defects

LO4.	Perform re-welding

### LO1.	MARK/LOCATE WELD DEFECTS

### ASSESSMENT CRITERIA:

- Location of weld defects identified/determined in accordance with industry standard.

- Weld defects marked for repair in accordance with industry standard.

- Procedures in locating weld defects performed as per approved procedures.

### CONTENTS:

- Types of welding defects

- Procedures in locating weld defects

- Proper uses of NDT equipment or tools

### CONDITION:

The students/trainees must be provided with:

- Equipment and accessories

- Tools

-	Chipping hammer

-	Steel brush

- Supplies/materials

-	Carbon steel plates

-	Pipe; alloy pipe

- Instructional materials

-  	Reference book/ modules/ learning guides/ video CDs,

-	Welding charts,

-   	Work plans

-    Drawing and specifications relevant to the task

### METHODOLOGIES:

- Lecture/ demonstrations

- Self-paced learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Return demonstration

### LO2.	PREPARE TOOLS AND EQUIPMENT

### ASSESSMENT CRITERIA:

- Tools and equipment are prepared appropriate to the job requirements

- Tools and equipment are properly checked to the job requirements

### CONTENTS:

  - Tools and equipment and their uses

  - Procedures in checking tools and equipment

### CONDITION:

The students/trainees must be provided with:

  - Equipment and accessories

  - Tools

-	Chipping hammer

-	Steel brush

-	Electric grinders

  - Supplies/Materials

- Carbon steel plates

- Cutting/ grinding disk

- Carbon steel plates

- Pipe

  - Instructional materials

-	Reference book/ modules/ learning guides/ video CDs,

-	Welding charts,

-	Work plans

-    Drawing and specifications relevant to the task

### METHODOLOGIES:

  - Lecture/ demonstrations

  - Self-paced learning

  - Group discussion

### ASSESSMENT METHODS:

  - Written/oral

  - Direct observation

  - Return demonstration

### LO3.	REMOVE DEFECTS

### ASSESSMENT CRITERIA:

- Weld defects removed/excavated in accordance with welding procedures.

- Removal of non-defective welds is minimized and cleaned.

- Visual and dye-penetrant test are performed to verify the extent of removal of defects

### CONTENTS:

- Dye penetrant testing principle and applications.

- Procedures of dye penetrant testing

- Weld defects removal and excavation

### CONDITION:

The students/trainees must be provided with:

- Tools

- Chipping hammers

- Steel brush

- Supplies/materials

- Developer

- Penetrant

- Cleaner

-	Cloth/ clean rag

- Instructional materials

-	Reference book/ modules/ learning guides/ video CDs

-   	Welding charts

-   	Work plans

-  	Drawing and specifications relevant to the task

### METHODOLOGIES:

- Lecture/ demonstrations

- Self-paced learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Return demonstration

### LO4.	PERFORM RE-WELDING

### ASSESSMENT CRITERIA:

- Re-welding performed in accordance with approved repair procedure.

- No new weld defects or damages occurred during re-welding.

- Weld visually checked after re-welding for acceptability

### CONTENTS:

- Rectifying weld defects

- Re-welding procedures

- Visual inspection of weld

### CONDITION:

The students/trainees must be provided with:

- Equipment and accessories

-	Welding machine with complete accessories

- Tools

-	Chipping hammers

-	Steel brush

-	Electric grinders

- Welding supplies/materials

-	Carbon steel plates

-	Cutting/ grinding disk

-	Welding consumables

### METHODOLOGIES:

- Lecture/ demonstrations

- Self-paced learning

- Group discussion

### ASSESSMENT METHODS:

- Written/oral

- Direct observation

- Return demonstration

MODULES OF INSTRUCTION

CORE COMPETENCIES

GAS TUNGSTEN ARC WELDING (GTAW) NC II

UNIT OF COMPETENCY	:	Weld Carbon Steel Plates

MODULE TITLE	:	PerformING Fillet Welding on Carbon Steel Plates

MODULE DESCRIPTOR	: 	This module covers fillet welding on carbon steel plates in all positions such as 1F, 2F, 3F, & 4F.

NOMINAL DURATION	:	50 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the trainee/student must be able to:

LO 1.  Weld carbon plates in flat position (IF)

LO 2.  Weld carbon steel plates in horizontal position (2F)

LO 3.  Weld carbon steel plates in vertical position (3F)

LO 4.  Weld carbon steel plates in overhead position (4F)

LO1.	Weld Carbon Steel Plates in Flat Position (1F)

### ASSESSMENT CRITERIA:

- Bead profile in accordance to WPS/ISO standard.

- Ripple regular in appearance achieved.

- Smoothness of joints and uniformity of finished beads attained.

- Work angle of TIG torch and filler rod observed and maintained in accordance to ISO standard.

- Leg size attained in accordance to WPS.

### CONTENTS:

- Essentials of welding

- International welding standard

- Weld profile

- Safe welding practices

- Welding techniques and procedures

### CONDITIONS:

### The student/trainee must be provided with the following:

- Equipment

-	Welding machine (AC or AC/DC)

-	Welding booth

-	Fumes exhauster

-	Welding table or jig

-	Portable grinder

- Tools/accessories

-	Set of box wrench

-	Welding mask

-	Chipping hammer

-	Steel brush

-	Dark glass

-	Clear glass

-	Weld gauge

-	Penlight

-	Dye penetrant (DPT) kit

-	Cutting/ grinding disk

-	Argon

-	Tig torch and accessories

-	Gas flowmeter

- Supplies/ materials

-	Tungsten electrode

-	Cutting grinding disk

-	Carbon steel plates

-	Filler wire

- Personal protective equipment

-	Safety shoes

-	Safety goggles

-	Apron

-	TIG gloves

-	Leggings

- Training materials

-	Welding manuals

-	Welding standards

-	Welding procedures specifications (WPS)

### METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

### ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO2.	Weld Carbon Steel Plates in Horizontal Position (2F)

### ASSESSMENT CRITERIA:

- Bead profile in accordance to WPS/ISO standard.

- Ripple regular in appearance achieved.

- Smoothness of joints and uniformity of finished beads attained.

- Work angle of TIG torch and filler rod observed and maintained in accordance to ISO standard.

- Leg size attained in accordance to WPS.

CONTENTS:

- Essentials of welding

- International welding standard

- Weld profile

- Safe welding practices

- Welding techniques and procedures

CONDITIONS:

The student/trainee must be provided with the following:

- Equipment

-	Welding machine (AC or AC/DC)

-	Welding booth

-	Fumes exhauster

-	Welding table or jig

-	Portable grinder

- Tools/accessories

-	Set of box wrench

-	Welding mask

-	Chipping hammer

-	Steel brush

-	Dark glass

-	Clear glass

-	Weld gauge

-	Penlight

-	Dye penetrant (DPT) kit

-	Cutting/ grinding disk

-	Argon

-	Tig torch and accessories

-	Gas flowmeter

- Supplies/ materials

-	Tungsten electrode

-	Cutting grinding disk

-	Carbon steel plates

-	Filler wire

- Personal protective equipment

-	Safety shoes

-	Safety goggles

-	Apron

-	TIG gloves

-	Leggings

- Training materials

-	Welding manuals

-	Welding standards

-	Welding procedures specifications (WPS)

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO3.	Weld Carbon Steel Plates in Vertical Position (3F)

ASSESSMENT CRITERIA:

- Bead profile in accordance to WPS/ISO standard.

- Ripple regular in appearance achieved.

- Smoothness of joints and uniformity of finished beads attained.

- Work angle of TIG torch and filler rod observed and maintained in accordance to ISO standard.

- Leg size attained in accordance to WPS.

CONTENTS:

- Essentials of welding

- International welding standard

- Weld profile

- Safe welding practices

- Welding techniques and procedures

CONDITIONS:

The student/trainee must be provided with the following:

- Equipment

-	Welding machine (AC or AC/DC)

-	Welding booth

-	Fumes exhauster

-	Welding table or jig

-	Portable grinder

- Tools/accessories

-	Set of box wrench

-	Welding mask

-	Chipping hammer

-	Steel brush

-	Dark glass

-	Clear glass

-	Weld gauge

-	Penlight

-	Dye penetrant (DPT) kit

-	Cutting/ grinding disk

-	Argon

-	Tig torch and accessories

-	Gas flowmeter

- Supplies/ materials

-	Tungsten electrode

-	Cutting grinding disk

-	Carbon steel plates

-	Filler wire

- Personal protective equipment

-	Safety shoes

-	Safety goggles

-	Apron

-	TIG gloves

-	Leggings

- Training materials

-	Welding manuals

-	Welding standards

-	Welding procedures specifications (WPS)

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

LO4.	Weld Carbon Steel Plates in Overhead Position (4F)

ASSESSMENT CRITERIA:

- Bead profile in accordance to WPS/ISO standard.

- Ripple regular in appearance achieved.

- Smoothness of joints and uniformity of finished beads attained.

- Work angle of TIG torch and filler rod observed and maintained in accordance to ISO standard.

- Leg size attained in accordance to WPS.

CONTENTS:

- Essentials of welding

- International welding standard

- Weld profile

- Safe welding practices

- Welding techniques and procedures

CONDITIONS:

The student/trainee must be provided with the following:

- Equipment

-	Welding machine (AC or AC/DC)

-	Welding booth

-	Fumes exhauster

-	Welding table or jig

-	Portable grinder

- Tools/accessories

-	Set of box wrench

-	Welding mask

-	Chipping hammer

-	Steel brush

-	Dark glass

-	Clear glass

-	Weld gauge

-	Penlight

-	Dye penetrant (DPT) kit

-	Cutting / grinding disk

-	Argon

-	Tig torch and accessories

-	Gas flowmeter

- Supplies/ materials

-	Tungsten electrode

-	Cutting grinding disk

-	Carbon steel plates

-	Filler wire

- Personal protective equipment

-	Safety shoes

-	Safety goggles

-	Apron

-	TIG gloves

-	Leggings

- Training materials

-	Welding manuals

-	Welding standards

-	Welding procedures specifications (WPS)

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

- Written/oral

- Interview

- Direct observation

UNIT OF COMPETENCY	:	Weld Carbon Steel Plates

MODULE TITLE	:	PerformING Groove Welding on Carbon Steel Plates

MODULE DESCRIPTOR	: 	This module covers groove welding on carbon steel plates in all position such as 1G, 2G, 3G & 4G.

NOMINAL DURATION	:	64 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the trainee/student must be able to:

LO1.	Weld carbon steel plates in flat position (IG)

LO2.	Weld carbon steel plates in horizontal position (2G)

LO3.	Weld carbon steel plates in vertical position (3G)

LO4.	Weld carbon steel plates in overhead position (4G)

LO1.	Weld Carbon Steel Plates in Flat Position (1G)

ASSESSMENT CRITERIA:

- Weldment of workpiece is free of defects.

- Weld size not greater than 2mm for side lap and 3 mm for crown height ( 1 mm.

- Weld profile according to WPS/industry standard.

- Penetration minimum of flush to base metal and convexity of not greater than 3mm in height, in accordance with WPS.

CONTENTS:

- Essentials of welding

- International welding standards

- Weld profile

- Bead profile a minimum flush to base metal

- Ripple regular in appearance

- Smoothness of joints

- Uniformity of finish beads

- Safe welding practices

- Welding techniques and procedures

CONDITIONS:

The student/trainee must be provided with the following:

- Equipment

- Welding machine (AC or AC/DC)

- Welding booth

- Fumes exhauster

- Welding table or jig

- Portable grinder

- Tools/Accessories

- Set of box wrench

- Welding mask

- Chipping hammer

- Steel brush

- Dark glass

- Clear glass

- Weld gauge

- Penlight

- Dye penetrant (DPT) kit

- Cutting/ grinding disk

- Argon

- Tig torch and accessories

- Gas flowmeter

- Supplies/ materials

- Tungsten electrode

- Cutting grinding disk

- Carbon steel plates

- Filler wire

- Personal protective equipment

- Safety shoes

- Safety goggles

- Apron

- TIG gloves

- Leggings

- Training Materials

- Welding manuals

- Welding standards

- Welding procedures specifications (WPS)

METHODOLOGIES:

- Lecture/demonstration

- Dualized

- Self-paced learning

ASSESSMENT METHODS:

Written/oral

Direct observation

Interview

LO2.	Weld Carbon Steel Plates in Horizontal Position (2G)

ASSESSMENT CRITERIA:

- Weldment of workpiece is free of defects.

- Weld size not greater than 2mm for side lap and 3 mm for crown height ( 1 mm.

- Weld profile  according to WPS/industry standard.

- Penetration minimum of flush to base metal and convexity of not greater than 3mm in height, in accordance with WPS.

CONTENTS:

Essentials of welding

International welding standards

Weld profile

- Bead profile a minimum flush to base metal

- Ripple regular in appearance

- Smoothness of joints

- Uniformity of finish beads

Safe welding practices

Welding techniques and procedures

CONDITIONS:

The student/trainee must be provided with the following:

Equipment

- Welding machine (AC or AC/DC)

- Welding booth

- Fumes exhauster

- Welding table or jig

- Portable grinder

Tools/accessories

- Set of box wrench

- Welding mask

- Chipping hammer

- Steel brush

- Dark glass

- Clear glass

- Weld gauge

- Penlight

- Dye penetrant (DPT) kit

- Cutting/ grinding disk

- Argon

- Tig torch and accessories

- Gas flowmeter

Supplies/ materials

- Tungsten electrode

- Cutting grinding disk

- Carbon steel plates

- Filler wire

Personal protective equipment

- Safety shoes

- Safety goggles

- Apron

- TIG gloves

- Leggings

Training materials

- Welding manuals

- Welding standards

- Welding procedures specifications (WPS)

METHODOLOGIES:

Lecture/demonstration

Dualized

Self-paced learning

ASSESSMENT METHODS:

Written/oral

Direct observation

Interview

LO3.	Weld Carbon Steel Plates in Vertical Position (3G)

ASSESSMENT CRITERIA:

1.	Weldment of workpiece is free of defects.

2.	Weld size not greater than 2mm for side lap and 3 mm for crown height ( 1 mm.

3.	Weld profile according to WPS/industry standard.

4.	Penetration minimum of flush to base metal and convexity of not greater than 3mm in height, in accordance with WPS.

CONTENTS:

Essentials of welding

International welding standards

Weld profile

- Bead profile a minimum flush to base metal

- Ripple regular in appearance

- Smoothness of joints

- Uniformity of finish beads

Safe welding practices

Welding techniques and procedures

CONDITIONS:

The student/trainee must be provided with the following:

Equipment

- Welding machine (AC or AC/DC)

- Welding booth

- Fumes exhauster

- Welding table or jig

- Portable grinder

Tools/accessories

- Set of box wrench

- Welding mask

- Chipping hammer

- Steel brush

- Dark glass

- Clear glass

- Weld gauge

- Penlight

- Dye penetrant (DPT) kit

- Cutting/ grinding disk

- Argon

- Tig torch and accessories

- Gas flowmeter

Supplies/ materials

- Tungsten electrode

- Cutting grinding disk

- Carbon steel plates

- Filler wire

Personal protective equipment

- Safety shoes

- Safety goggles

- Apron

- TIG gloves

- Leggings

Training materials

- Welding manuals

- Welding standards

- Welding procedures specifications (WPS)

METHODOLOGIES:

Lecture/demonstration

Dualized

Self-paced learning

ASSESSMENT METHODS:

Written/oral

Direct observation

Interview

LO4.	Weld Carbon Steel Plates in Overhead Position (4G)

ASSESSMENT CRITERIA:

1.	Weldment of workpiece is free of defects.

2.	Weld size not greater than 2mm for side lap and 3 mm for crown height ( 1 mm.

3.	Weld profile according to WPS/industry standard.

4.	Penetration minimum of flush to base metal and convexity of not greater than 3mm in height, in accordance with WPS.

CONTENTS:

Essentials of welding

International welding standards

Weld profile

- Bead profile a minimum flush to base metal

- Ripple regular in appearance

- Smoothness of joints

- Uniformity of finish beads

Safe welding practices

Welding techniques and procedures

CONDITIONS:

The student/trainee must be provided with the following:

Equipment

- Welding machine (AC or AC/DC)

- Welding booth

- Fumes exhauster

- Welding table or jig

- Portable grinder

Tools/accessories

- Set of box wrench

- Welding mask

- Chipping hammer

- Steel brush

- Dark glass

- Clear glass

- Weld gauge

- Penlight

- Dye penetrant (DPT) kit

- Cutting/ grinding disk

- Argon

- Tig torch and accessories

- Gas flowmeter

Supplies/ materials

- Tungsten electrode

- Cutting grinding disk

- Carbon steel plates

- Filler wire

Personal protective equipment

- Safety shoes

- Safety goggles

- Apron

- TIG gloves

- Leggings

Training materials

- Welding manuals

- Welding standards

- Welding procedures specifications (WPS)

METHODOLOGIES:

Lecture/demonstration

Dualized

Self-paced learning

ASSESSMENT METHODS:

Written/oral

Direct observation

Interview

UNIT OF COMPETENCY	:	Weld Carbon Steel PIPES

MODULE TITLE	:	PerformING Groove Welding on Carbon Steel Pipes

MODULE DESCRIPTOR	:	This module covers groove welding on carbon steel pipes in all position such as 2G, 5G & 6G.

NOMINAL DURATION	:	80 hours

SUMMARY OF LEARNING OUTCOMES:

Upon completion of this module the trainee/student must be able to:

LO1.	Weld carbon steel pipes in horizontal position (2G)

LO2.	Weld carbon steel pipes in horizontal fixed position (5G)

LO3.	Weld carbon steel pipes in 45( fixed position (6G)

LO1.	Weld Carbon Steel Pipes in HORIZONTAL Position (2G)

ASSESSMENT CRITERIA:

- Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

- concavity

- convexity

- undercut

- excess penetration

- lack of fusion

- burn-through

- cracks

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

Essentials of welding

International welding codes and standards

Acceptable weld profiles

Weld defects, causes and remedies

Welding Procedure Specifications (WPS)

Welding techniques and procedures

Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

Equipment

- Welding machine (DC)

- Welding booth

- Fumes exhauster

- Welding table or jig

Tools/accessories

- Welding mask

- Chipping hammer

- Steel brush

- Dark glass

- Clear glass

- Gas Flowmeter

- Tig torch set

- Portable grinder

Supplies/ materials

- Filler rods

- Tungsten electrode

- Cutting/ grinding disk

- Carbon steel pipes

- Argon gas

Personal protective equipment

- Safety shoes

- Safety goggles

- Apron

- Tig gloves

- Leggings

Training materials

- Welding manuals

- Welding standards

- Welding procedures specifications (WPS)

METHODOLOGIES:

Lecture/demonstration

Dualized

Self-paced learning

ASSESSMENT METHODS:

Written/oral

Direct observation

Interview

LO2.	Weld Carbon Steel Pipes in Horizontal FIXED Position (5G)

ASSESSMENT CRITERIA:

- Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

- concavity

- convexity

- undercut

- excess penetration

- lack of fusion

- burn-through

- cracks

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

Essentials of welding

International welding codes and standards

Acceptable weld profiles

Weld defects, causes and remedies

Welding procedure specifications (WPS)

Welding techniques and procedures

Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

Equipment

- Welding machine (DC)

- Welding booth

- Fumes exhauster

- Welding table or jig

Tools/accessories

- Welding mask

- Chipping hammer

- Steel brush

- Dark glass

- Clear glass

- Gas flowmeter

- Tig torch set

- Portable grinder

Supplies/ material

- Filler rods

- Tungsten electrode

- Cutting/ grinding disk

- Carbon steel pipes

- Argon gas

Personal protective equipment

- Safety shoes

- Safety goggles

- Aapron

- Tig gloves

- Leggings

Training materials

- Welding manuals

- Welding standards

- Welding procedures specifications (WPS)

METHODOLOGIES:

Lecture/demonstration

Dualized

Self-paced learning

ASSESSMENT METHODS:

Written/oral

Direct observation

Interview

LO3.	Weld Carbon Steel Pipes in 45( fixed Position (6G)

ASSESSMENT CRITERIA:

- Root penetration not exceeding allowable tolerances specified by welding codes/ standards on

- concavity

- convexity

- undercut

- excess penetration

- lack of fusion

- burn-through

- cracks

- Weld capping/ final pass not exceeding allowable tolerances specified by welding codes/ standards on

- height of reinforcement

- underfill

- porosities

- undercut

- cracks

- cold laps

- Uniformity of bead ripples must be in accordance with welding standards

- Stringer or layered beads deposited in accordance with welding standards

- Finish weldment visually acceptable in accordance with welding standards for:

- spatters

- arc strikes

- slag

- uniformity of beads

CONTENTS:

Essentials of welding

International welding codes and standards

Acceptable weld profiles

Weld defects, causes and remedies

Welding procedure specifications (WPS)

Welding techniques and procedures

Safe welding practices

CONDITIONS:

The student/trainee must be provided with the following:

Equipment

- Welding machine (DC)

- Welding booth

- Fumes exhauster

- Welding table or jig

Tools/accessories

- Welding mask

- Chipping hammer

- Steel brush

- Dark glass

- Clear glass

- Gas Flowmeter

- Tig torch set

- Portable grinder

Supplies/ materials

- Filler rods

- Tungsten electrode

- Cutting/ grinding disk

- Carbon steel pipes

- Argon gas

Personal protective equipment

- Safety shoes

- Safety goggles

- Apron

- Tig gloves

- Leggings

Training materials

- Welding manuals

- Welding standards

- Welding procedures specifications (WPS)

METHODOLOGIES:

Lecture/demonstration

Dualized

Self-paced learning

ASSESSMENT METHODS:

Written/oral

Direct observation

Interview

# What is Competency-Based Curriculum (CBC)

- A competency-based curriculum is a framework or guide for the subsequent detailed development of competencies, associated methodologies, training and assessment resources.

- The CBC specifies the outcomes which are consistent with the requirements of the workplace as agreed through the industry or community consultations.

- CBC can be developed immediately when competency standards exist.

- When competency standards do not exist, curriculum developers need to clearly define the learning outcomes to be attained. The standard of performance required must be appropriate to industry and occupational needs through the industry/enterprise or specified client group consultations.

These materials are available in both printed and electronic copies.

For more information please contact:

Technical Education and Skills Development Authority (TESDA)

Telephone Nos.: 893-8281, 817-4076 to 82 loc. 611 to 630, 631 and 635 or visit our website: www.tesda.gov.ph or the TESDA Regional or Provincial Office nearest you.